## Slide 1: SCWR Fuel Rod Design Requirements
  Design Limits Input for Performance Evaluations
  H. Garkisch, Westinghouse Electric Co.

## Slide 2: SCWR Fuel Rod Design Requirements - Overview -
The primary function of the fuel rod is to generate and transfer heat to the reactor coolant.
A second function of the fuel is to contain the fuel and the fission products and provide a barrier against coolant contamination with fission products. For this the structural integrity of the fuel rod must be maintained in compliance with applicable requirements.
The SCWR operating conditions exceeds the current experience with LWRs and LMFBRs, thus specific criteria must be developed.

## Slide 3: SCWR Fuel Rod Design Requirements - Overview -
Generic Considerations for SCWR developed during 1st year of NERI program:
  Compile NRC SRP criteria for nuclear reactors
  Identify main areas of difference between SCWR and standard criteria
  Identify simplified requirements for preliminary analysis
Proposal for specific design criteria/fuel rod failure modes developed and submitted to INEEL during 2nd year
  Develop detailed review of NRC SRP Criteria
  Develop specific fuel failure modes and design criteria for SCWR

## Slide 4: Design Criteria: LWR experience
Fuel Design requirements for LWRs are defined in the NRC Standard Review Plan to satisfy 10CFR50 GDC10
“The objectives of the fuel system safety review are to provide assurance that
  (a) the fuel system is not damaged as a result of normal operation and anticipated operational occurrences,
  (b) fuel system damage is never so severe as to prevent control rod insertion when it is required,
  (c) the number of fuel rod failures is not underestimated for postulated accidents, and
  (d) coolability is always maintained.”

## Slide 5: Design Criteria: LWR experience

## Slide 6: Design Criteria for SCWRs

## Slide 7: Fuel Rod Failure Modes
    Fracture induced by rod pressure and fuel cladding mechanical interaction, assisted by irradiation assisted stress corrosion cracking and stress corrosion induced embrittlement of the cladding.
    Creep rupture burst due to over-pressure or sustained stress induced by fuel-cladding differential thermal expansion.
    Cladding failure induced by fuel cladding mechanical interaction during steady state and then transient operation at high burn-up.
    Cladding fatigue failure, an unlikely failure mode for a reactor in base load operation.
    Excessive cladding growth and swelling exceeding the functional constraints of the fuel assembly, an unlikely failure mode in a thermal flux operating environment.
    Cladding corrosion, which thins the cladding and increases cladding temperatures, is unknown in a supercritical steam environment. A thick corrosion layer on the cladding increases cladding and fuel temperatures and can induce failure. Due to the high system operating pressure cladding collapse under external differential pressure.
    Cladding collapse under external differential pressure

## Slide 8: Fuel Rod Design Criteria Basis
    NUREG-0800, STANDARD REVIEW PLAN, NUCLEAR REGULATORY COMMISSION
      Criteria Summarized in Three Tables (Fuel Rod Damage, Fuel Rod Failure, Core Coolability).
    ASME B&PV Code Section III Article NH-3000
      The fuel rod cladding is not covered by the code.
      However, by applying criteria based on the code approach, a design finds acceptance without further justification.

## Slide 9: SCWR Criteria Issues
At super critical steam temperature (> 800 0F) ASME high temperature design rules apply;
Creep, irradiation and thermal creep must be checked or considered;
The high system pressure requires check of buckling and stress at depressurization.

## Slide 10: ROD INTERNAL PRESSURE CRITERION
The rod internal pressure of the lead rod in the reactor shall not exceed the pressure that could:
  Cause the diametral gap between the fuel and the cladding to increase due to steady state operation, cause ballooning and affect the coolant flow;
  Exceed the rupture pressure of the cladding (if known);
  Local overheating of the cladding.
Notes: <number>
<footer>
<header>
<date/time>

## Slide 11: CLADDING STRESS CRITERION Criterion, Basis, Implementation
Cladding Stress Criterion: Where creep is significant, the ASME B&PV Code Section III Article NH-3000 specifies that the strain limiting criteria, rather than stress limiting criteria are applied. However, simplified methods can be used to establish conservative limits for stress.
yield stress
Sm = min. of | 2/3 Sy at ambient (room) temperature
| 2/3 Sy at service temperature
| 1/3 Sult at ambient (room) temperature
| 1/3 Sult at service temperature
stress rupture
St = min. of | 100 % of the stress to cause 1% strain.
| 80% of the stress to initiate tertiary creep,
| 67% of the minimum stress to cause rupture

## Slide 12: CLADDING STRESS CRITERION (Condition I) Criterion, Basis, Implementation
Cladding Stress Criteria: The time independent stress limits for the load categories are as follows:
With: Pm, primary membrane stress (dP across the cladding and PCI); Pl primary local stress (stress raiser due to pellet cracking and bambooing); Pb, primary bending stress (bowing or PCI gradients); and Q, secondary stress (thermal stresses)
      Sin (Pm) < 1.0 Sm
      Sin (Pm + Pl) < 1.5 Sm
      Sin (Pm + Pl + Pb) < 1.5 Sm
      Sin (Pm + Pl + Pb+ Q) < 3.0 Sm
The stress adder Q is included to assure that the transient thermal stresses do not exceed stresses which could exhaust the deformation capability of materials
Typical fuel performance codes (like FRAPCON) calculate Pm and Q, not Pl and Pb.
The time dependent stress limit is as follows: <D
Basis:
Table 3, Paragraphs a; SRP II, A-1-a
ASME B&PV Code, Section III, Division 1, Article NH-3000
ASME B&PV Code, Section III, Article III-2000, III-2100

## Slide 13: CLADDING STRAIN CRITERION (Condition I and II)
The total permanent uniform strain shall not exceed:
  1 % membrane strain (limiting)
  2 % bending strain
  5 % local strain
The intent of this requirement is to limit cladding damage due to slow rate strain accumulation at which the stress does not reach the stress limit (yield stress). The clad loading mechanism is the rod internal differential pressure with the system pressure and clad straining by the pellet expansion and PCI.
A bending strain and local strain are not calculated by FRAPCON and the limits are not applied at this time.
Basis:
  Table 3, Paragraph a, and SRP II, A-1-a
  ASME B&PV Code Section III Article NH-3000

## Slide 14: FUEL TEMPERATURE CRITERION
During Condition I and Condition II events the peak kw/ft fuel rods shall not exceed the UO2 melting temperature with 95%/95% probability and confidence level.
The un-irradiated fuel melting temperature is 2805 0C. It reduces by 58 0C for every 10000 MWd/MTU burnup. For rods with Gadolinia the melting temperature is reduced 3.75 0C for each w/0 Gadolinia oxide.
  For preliminary design purposes of high burnup fuel limit the maximum fuel temperature to < 2600 0C

## Slide 15: CORROSION AND FATIGUE CRITERIA
Corrosion:
  Cladding corrosion reduces the effective thickness of the cladding, decreases the effective thermal conductivity of the cladding and thus increases the cladding and fuel temperatures.
  In absence of any data a conservative linear increase of the corrosion layer of 0.1 mm (4 mil) shall be assumed.
Cladding Fatigue:
  Cumulative number of strain cycles shall be less than the design fatigue lifetime with appropriate margins.
    The cumulative number of strain cycles shall be less than the design fatigue lifetime, with a safety factor of 2 on stress amplitude and a safety factor of 20 on the number of cycles
Notes: <number>
<footer>
<header>
<date/time>

## Slide 16: CLAD COLLAPSE AND ROG GROWTH
Clad Collapse:
  The clad shall be free standing at BOL (before densification)
  No clad collapse in the gas plenum region
  No clad collapse into gaps between pellets
  At high temperatures elastic, plastic and potential creep deformation must be considered as well as the tube ovality.
Rod Growth:
  Fuel rod length changes due to irradiation effects and differential thermal expansion shall not cause interference with the fuel Assembly Structure
  From the fuel cladding expansion, thermal swelling and creep the total length change of the cladding can be estimated with the axial temperature and axial growth profile as input. Similar calculations are required to estimate the growth of the assembly structure. The differential between both must show a gap between the rod length and the assembly structure.This evaluation is a critical design input because it determines the assembly length.

## Slide 17: OTHER CRITERIA
End Plug Weld Stress Criterion
Fuel Rod Length Change Criterion

## Slide 18: MA956 is not isotropic

## Slide 19: Design Criteria and Evaluation
Available material properties for MA956, other ODS and high Nickel materials are spotty and not consistent
Irradiated properties are largely missing
Guesses of some properties and limits are required
A systematic compilation of material properties required